MAGNESIUM CHLORIDE SOLUTION (LIQUID)
	ELEMENT
	ANALYSIS RESULTS

	OBé
	30

	Conc. Of MgCl2
	29% Min

	Conc. Of CaCl2
	1% Max

	Conc. Of NaCl2
	0.2% Max

	PH
	7


Packing: In 1 ton IBCS

