MAGNESIUM OXIDE POWDER
	ELEMENT
	ANALYSIS RESULT

	MgO
	80-82%

	CaO
	6-8%

	Fe2O3
	0.40-0.60%

	Al2O3
	0.00%

	SiO2
	4-6%

	L.O.I
	5-7%


[image: image1.jpg]



· Particle size: Passing through 200 mesh sieve (75 micron) 
· Packing : Poly propylene bags : 25 kg  bags &  jumbo bag.
